# FiberTite 200 Fascia System: Fully Adhered, Mechanically Attached or Stone Ballast Version

SECTION 07710

## PART ONE GENERAL

  - SUMMARY:

- Work included: Furnishing and installing factory fabricated and finished roof edging.

- Related Work: [Insert applicable sections].

  - REFERENCES:

- Factory Mutual Research Corporation (FMRC), P.O. Box 9102, Norwood, MA 02082, 617-762-4300.

- SPRI Sheet Membrane & Component Suppliers to the Commercial Roofing Industry, 175 Highland Ave., Needham, MA 02194, 617-444-0242, fax: 617-444-6111.

  - SUBMITTALS:

- Product Data: Provide manufacturer’s product and complete installation data for all materials in this specification.

- Shop Drawings: Show profiles, joining method, location of accessory items, anchorage and flashing details, adjacent construction interface, and dimensions.

- Samples: Available upon request; size to adequately represent material.

- Installation Guide: The product manufacturer shall provide a written installation guide.

  - QUALITY ASSURANCE:

- High performance roof edge system shall be CERTIFIED by the manufacturer to comply with ANSI/SPRI Standard ES-1-98. Roof edge shall meet performance design criteria according to the following test standards: [select, if applicable]:

1.	ANSI/SPRI ES-1 Test Method RE-1 Test for Roof Edge Termination of Single-Ply Roofing Membranes: The fascia system shall be tested to secure the membrane to minimum of 100 lbs/ft in accord with the ANSI/SPRI ES-1 Test Method RE-1. Use the current edition of ANSI/SPRI ES-1 Wind Design Standard for Edge Systems Used with Low Slope Roofing Systems.

- ANSI/SPRI ES-1 Test Method RE-2 Pull-Off Test for Fascia: The fascia system shall be tested in accord with the ANSI/SPRI ES-1-98 Test Method RE-2. Use the current edition of ANSI/SPRI ES-1 Wind Design Standard for Edge Systems Used with Low Slope Roofing Systems.

3.	The fascia product shall be listed in current Factory Mutual Research Corporation Approval Guide approved for [Select FM 1-90 through FM 1-195]. Consult current FM Approval Guide or contact the factory.

  - PRODUCT HANDLING:

- All material shall arrive in the manufacturer’s original sealed, labeled containers.

- Store materials in a dry, protected, well-vented area. The contractor shall report damaged material immediately to the delivering carrier and note such damage on the carrier’s freight bill of lading.

- Remove protective plastic surface film immediately before installation.

  - SUBSTITUTIONS:

- Proposals for substitution products shall be accepted only from bidding contractors a minimum of 10 working days before bid due date. The proposed substitution shall meet the performance and quality standards of this specification (see section 1.04).

  - JOB CONDITIONS:

- Verify that other trades are complete before installing the roof edging.

- Mounting surfaces shall be straight and secure; substrates shall be of proper width.

- Refer to the construction documents, shop drawings and manufacturer’s installation instructions.

- Coordinate installation with roof membrane manufacturer’s installation instructions.

- Observe all appropriate OSHA safety guidelines for this work.

  - WARRANTY/GUARANTEE:

- Provide a FiberTite’s full system warranty for roof edge system when installed per FiberTite’s instructions.

- Provide a 20 year warranty for painted finish covering color fade, chalk and film integrity.

## PART TWO PRODUCTS

  - MANUFACTURER:

- FiberTite, Inc.

1600 Airport Road

Waukesha, WI 53188

262-549-6900

Fax: 262-549-6009

Internet address: www.metalera.com/fibertite

  - ROOF EDGING SYSTEM:

- FiberTite 200 Fascia: Decorative metal fascia with continuous galvanized steel waterdam to terminate single-ply roofing at perimeter. The system shall be watertight with concealed splice plates and no exposed fasteners. Model(s) shall be [choose one].

- For standard sizes with 2” rise above the roof edge for all membrane attachments: (FA-F50, FA-F65, FA-F80, FA-F95, FA-F110, FA-F125). Fascia model numbers denote inches; (i.e. FA-F50 has a 5” face height).

- Custom sizes by request.

- PERFORMANCE CHARACTERISTICS:

- Roof edging shall lock membranes, preventing wind pullback.

- Fascia shall freely thermal cycle on waterdam, preventing periodic maintenance.

- Fascia may be factory modified for true radius application.

- Fascia metal gauge [choose]: .040”, .050”, or .063” thick formed aluminum; or 22 gauge or 24 gauge galvanized steel with Kynar 500 finish.

- Fascia: standard 12’-0” (3.65 m) lengths with matching concealed joint splice plates.

- Waterdam: Shall be continuous 24 gauge commercial type G-90 galvanized steel at 12’-0” (3.65 m) standard lengths.

- Fasteners: 1-1/4” ring shank nails provided. No exposed fasteners permitted.

- Exterior fascia finishes: [For aluminum choose] Natural mill finish, Kynar 500 from manufacturer’s standard colors, custom color Kynar 500, or Clear or Color Anodized. [For 22 gauge or 24 gauge galvanized steel choose] Kynar 500 standard color from manufacturer’s standard colors.

  - ACCESSORIES:

- Corners, fascia scuppers, spillouts, etc. shall be fabricated by manufacturer. Factory fabricated, mitered corners shall have 14” nominal (356 mm) leg lengths.

- Provide matching ledgecaps, downspouts, or other special fabrications as detailed.

## PART THREE EXECUTION

  - INSPECTION:

- Verify that the roof edging installation will not disrupt other trades. Verify that the substrate is dry, clean and free of foreign matter. Report and correct defects prior to any installation.

  - INSTALLATION OF FIBERTITE 200 ROOF EDGING SYSTEM:

- Submit product design drawings for review and approval to Architect or Specifier before fabrication.

- Installing contractor shall check as-built conditions and verify the FiberTite’s roof edge details for accuracy to fit the wall assembly prior to fabrication. The installer shall comply with FiberTite’s installation guide when setting edging.

- Roofing membrane must be single-ply; not to exceed 60 mils (1.6 mm) thick.

- Installer shall use provided fasteners consistent with FiberTite’s instructions; suitable for the substrate to which being installed.

END OF SECTION 07710